## Slide 1: CHRONOS Meeting
Julian Geiger
jgeiger@iciq.es
THEOS@EPFL
11/04/2023

## Slide 2: Structural overview
Julian Geiger
CHRONOS Meeting, 11/04/2023
System | Unit formula | Cell formula | # Atoms | # Conf. | Uinit / eV
Mn-olivine | LiMnPO4 | Mn4O16P4Li4 | 28 | 7 (1), 249 (2) | ~5.5 (4.6-6.3)
Fe-olivine | LiFePO4 | Fe4O16P4Li4 | 28 | 10 (1), 462 (2) | ~5.3 (5.3-5.4)
Mn/Fe-olivine | LiMn0.5Fe0.5PO4 | Mn2Fe2O16P4Li4 | 28 | 16 (1), 840 (2) | as above
Mn-spinel | LiMn2O4 | Mn16O32Li8 | 56 | 76 (1) | ~6.6 (6.2-6.8)
Mn/Ni-spinel | LiMn1.5Ni0.504 | Mn12Ni4O32Li8 | 56 | 22 (1), 5858 (2) | Mn: ~6.6 (6.6-7.0) Ni: ~8.1 (6.8-9.4)

## Slide 3: Structural overview
Julian Geiger
CHRONOS Meeting, 11/04/2023
Example for Mn-olivine:

## Slide 4: Structural overview
Julian Geiger
CHRONOS Meeting, 11/04/2023
Example for Mn-olivine:

## Slide 5: Structural overview
Julian Geiger
CHRONOS Meeting, 11/04/2023
Example for Mn-olivine:

## Slide 6: Structural overview
Julian Geiger
CHRONOS Meeting, 11/04/2023
Example for Mn-olivine:

## Slide 7: Using the workchain
Julian Geiger
CHRONOS Meeting, 11/04/2023
Thus far
Resolved issue with atom ordering
Custom magnetic ordering (e.g. AFM)
Going forward
Full infrastructure available to create HTP data for ML
Influence of Li distribution on intercalation voltages
Influence of magnetic ordering on U+V values